## Company Name.

# Cancrie Pvt. Ltd.

## Manufacturing Plant Address

F-2312, Goner Road, Ramchandrapura Industrial Area,
Vidhani, Jaipur, Rajasthan, 302022, India

## Founders

### Dr. Akshay Jain

Co-founder, CEO
PhD in Chemical Engineering, National University of Singapore (NUS), Singapore
Inventor with 1 patent and author of 15 research publications.

Mahi Singh

Co-founder, COO

MS International Studies,
NTU, Singapore
9+ years in Business & Strategy
Climate Coach | Serial Entrepreneur

## Contacts

Phone number: +91-8287695157
Email: business@cancrie.co

# Overview

Cancrie develops patented advanced nanocarbons engineered for life enhancement and performance efficiency improvements in batteries and capacitors.

Built on 13+ years of hands-on research and innovation, our technology transforms biomass into high-performance materials using sustainable and smarter processing methods.

Our solutions are designed for seamless integration in the batteries, without requiring major process changes.

So Cancrie is creating a sustainable supply chain for high-performing batteries.

# Vision: S.E.T

## Sustainability

We are advancing sustainability by helping the world achieve net-zero emissions through circular manufacturing — enabling complete chemical recovery, total heat recovery, and zero discharge processes.

## Efficiency

Cancrie is improving efficiency by enabling higher-performing energy storage devices through a simple and scalable drop-in solution.

## Transformation

We are driving transformation by converting waste into high-value products, giving millions of tonnes of waste a second life, reducing dependence on incineration and landfills, and powering next-generation energy storage devices.

# Key Advantages

## 01. Better Process

Up to 89% lower energy consumption, 20× lower greenhouse gas emissions, and significantly reduced processing temperatures through optimized carbon manufacturing.

## 02. Superior Carbon Performance

Engineered nanocarbon materials with enhanced cohesive strength and improved electrochemical performance for high-performing batteries.

## 03. Improved Battery Output

Higher charge acceptance, extended battery life, and reduced warranty failures across lead-acid and advanced energy storage systems.

## 04. Sustainable by Design

Biomass-derived nanocarbons providing a cleaner, circular alternative to conventional petroleum-based carbon materials.

# Supported Battery Chemistries

## Lead-Acid Batteries

Cancrie nanocarbon materials are designed to improve charge acceptance, reduce sulfation, enhance conductivity, improve active material bonding, and extend cycle life in lead-acid battery systems.

### Supported applications include:

- tubular batteries

- solar batteries

- inverter batteries

- automotive batteries

- start-stop batteries

- VRLA batteries

- e-rickshaw batteries

### Key benefits include:

- higher charge acceptance

- improved lifecycle performance

- reduced negative plate shedding

- improved deep discharge performance

## Lithium-ion Batteries

Cancrie nanocarbon materials function as cathode-enhancing additives designed to improve electrochemical reaction efficiency, ion transport, thermal stability, and energy density in lithium-ion battery systems.

### Key benefits include:

- improved energy density

- enhanced power performance

- improved thermal stability

- lower dependence on critical mineral usage

- compatibility with existing manufacturing processes

### Supported applications include:

- EV batteries

- energy storage systems

- portable energy storage devices

## Sodium-ion Batteries

Cancrie nanocarbon materials are engineered to address slow ion kinetics and electrode degradation challenges commonly found in sodium-ion battery systems.

### Key benefits include:

- improved ion transport

- enhanced structural stability

- improved power delivery

- extended cycle life

- improved thermal safety

## Redox Flow Batteries

Cancrie nanocarbon materials function as surface-activating electrode materials designed to improve electrochemical activity and reduce internal resistance in redox flow battery systems.

### Key benefits include:

- improved electron transfer efficiency

- reduced voltage losses

- improved round-trip efficiency

- enhanced electrochemically active surface area

## Supercapacitors

Cancrie nanocarbon materials are designed to improve charge-storage capacity and power delivery through engineered pore structures and enhanced electrochemical surface area.

### Key benefits include:

- higher power density

- lower internal resistance

- rapid charge-discharge capability

- improved energy retention

## Fuel Cells

Cancrie nanocarbon materials provide conductive and corrosion-resistant frameworks designed to improve catalyst utilization and electrochemical conversion efficiency in fuel cell systems.

### Key benefits include:

- improved catalyst distribution

- enhanced mass transport

- improved power output

- reduced precious metal loading requirements

- improved system durability

# Applications

Cancrie nanocarbon materials are designed for energy storage systems requiring high reliability, performance efficiency, scalability, and long operational life.

## Mobility

Advanced nanocarbon materials designed for transportation and high-performance mobility systems.

### Electric Vehicles (EVs)

- high energy density

- high power density

- stable cycling performance

### E-Rickshaws

- cost-efficient performance

- reliable daily operation

- optimized for frequent charging cycles

### Drones

- lightweight energy systems

- high power delivery

- consistent output performance

### Forklifts & Industrial Vehicles

- high cycle durability

- consistent performance under load

- designed for intensive duty cycles

## Stationary Energy

Energy storage materials designed for continuous operation and backup power systems.

### Solar Energy Storage

- efficient energy storage

- reliable charge-discharge performance

- supports renewable energy integration

### UPS Systems

- instant power delivery

- high reliability

- stable operational performance

### Telecom Infrastructure

- long-duration backup support

- low maintenance requirements

- consistent field performance

# Lead-Acid Battery Performance Data

Validated by ARAI and third-party accredited laboratories. Proven across more than 20 battery manufacturers.

## Fast Charge Capability

### Stable Fast Charging

- Stable charging performance up to 0.22C charging rates

- No material degradation during fast charging conditions

## Enhanced Capacity Across C-Rates

Cancrie nanocarbon demonstrated 10–20% higher discharge capacity across multiple discharge rates.

### High Rate Discharge Performance

| Discharge Rate | Capacity |
| --- | --- |
| C5 Rate | 92.6% |
| C3 Rate | 80.65% |
| C2 Rate | 72.2% |
| C1 Rate | 57% |

## Ampere-Hour (Ah) Efficiency

- Up to 98% Ah efficiency

- Minimal charge loss

- Improved electrochemical stability

- Strong cycle life performance

## Watt-Hour (Wh) Efficiency

- Up to 85% Wh efficiency

- Improved usable energy output

- Enhanced system efficiency

# FESEM Surface Structure Analysis

## Cancrie Nanocarbon

- Better active material bonding

- Improved structural integrity

- Reduced negative plate shedding

- Longer operational life

## Conventional Carbon Black

- Lesser active material bonding

- Higher material shedding

- Reduced operational life

# Differential Performance

## Cancrie Higher Carbon vs Conventional Battery Carbon

### Higher Volume

Cancrie nanocarbon demonstrated approximately 3× greater volume compared to conventional battery carbon materials.

### Improved Conductivity

Higher volume structure improves conductivity and energy storage performance.

### Reliable Power Delivery

Improved structural properties support stable power delivery under heavy load conditions.

# Deep Discharge Cycling Performance

## Tubular Flooded Batteries (Solar & Inverter Applications)

Life cycle performance at 80% depth of discharge (DOD) and C10 discharge rate improved significantly using Cancrie nanocarbon materials.

| Battery Type | Deep Discharge Cycles |
| --- | --- |
| Cancrie Nanocarbon Battery | ~1100 cycles |
| Regular Carbon Battery | ~900 cycles |

### Warranty Impact

- Warranty period increase: 3–12 months

- Depends on application conditions

### Additional Observations

- No negative plate shedding observed after 1100 cycles using Cancrie nanocarbon

- Heavy shedding observed after 900 cycles using conventional carbon black

# Charge Acceptance Performance

## Motor Vehicle Starting Batteries

### Charge Acceptance Test (IEC 60095)

| Battery Type | Current After 10 min | Amp Hour After 10 min |
| --- | --- | --- |
| Control Battery | 20.3 A | 3.6 Ah |
| Cancrie Nanocarbon Battery | 32.8 A | 5.76 Ah |

### Performance Improvement

- Up to 60% higher charge acceptance

# Fast Charging Validation

## Capacity Retention Across Charging Rates

| Charging Rate | Battery with Carbon Black | Battery with Cancrie Nanocarbon |
| --- | --- | --- |
| 0.12 C | 100% | 100% |
| 0.14 C | 98% | 100% |
| 0.16 C | 91% | 100% |
| 0.18 C | 84% | 100% |
| 0.25 C | 82% | 100% |

# Laboratory Validation

- ARAI validated

- Tested at third-party NABL accredited laboratories

- Proven across industrial-scale battery manufacturing environments

## Lithium-ion Batteries

### Lithium-ion Battery Solutions

Cancrie’s biomass-derived nanocarbon materials function as high-efficiency cathode-enhancing additives designed to improve electrochemical reactions, energy density, ion transport, and power performance in lithium-ion battery systems.

The materials are designed as drop-in compatible solutions that integrate into existing manufacturing lines without requiring major process modifications.

### Key benefits include:

- improved energy density

- enhanced power performance

- improved ion transport

- improved thermal stability

- safer battery operation

- longer cycle life

- reduced dependence on critical mineral mining

- lower carbon footprint in battery production

## Sodium-ion Batteries

### Sodium-ion Battery Solutions

Cancrie nanocarbon materials are engineered to address slow ion kinetics and electrode degradation challenges commonly associated with sodium-ion battery systems.

The high-surface-area nanocarbon framework facilitates ion transport and improves structural stability during repeated charge-discharge cycles.

### Key benefits include:

- improved ion transport

- enhanced structural integrity

- improved power delivery

- longer cycle life

- improved thermal safety

- reduced lithium and cobalt dependency

- lower environmental impact

- cost-effective energy storage performance

## Redox Flow Batteries

### Redox Flow Battery Solutions

Cancrie nanocarbon materials function as high-performance surface activators designed to improve electrochemical activity and reduce internal resistance at the electrode-electrolyte interface in redox flow battery systems.

The engineered nanocarbon structure increases electrochemically active surface area and accelerates electron transfer processes.

### Key benefits include:

- improved redox kinetics

- reduced voltage losses

- improved round-trip efficiency

- enhanced electrochemically active surface area

- compact and cost-effective system design

- reduced dependence on petroleum-based catalysts

- reduced rare-metal additive requirements

## Supercapacitors

### Supercapacitor Solutions

Cancrie nanocarbon materials are designed to improve charge-storage capacity and power delivery through engineered pore architecture and enhanced electrochemical surface area.

The materials enable rapid electrolyte penetration and reduced internal resistance for high-performance energy delivery applications.

### Key benefits include:

- higher power density

- improved energy retention

- reduced internal resistance

- rapid charge-discharge capability

- improved thermal performance

- compact device architecture

- sustainable alternative to petroleum-based activated carbon

### Supported applications include:

- regenerative braking systems

- grid stabilization

- rapid-response industrial systems

## Fuel Cells

### Fuel Cell Solutions

Cancrie nanocarbon materials provide conductive and corrosion-resistant frameworks designed to improve catalyst utilization, mass transport, and electrochemical conversion efficiency in fuel cell systems.

The engineered nanocarbon structure improves catalyst distribution and electrochemically active surface area for enhanced system performance.

### Key benefits include:

- improved catalyst utilization

- enhanced mass transport

- higher power output

- extended system durability

- reduced precious metal loading

- reduced petroleum-based component dependency

- improved sustainability in fuel cell manufacturing

### Supported applications include:

- heavy-duty transportation

- stationary power systems

- clean energy infrastructure

# Research & Validation

Cancrie nanocarbon materials have been validated by ARAI and third-party NABL accredited laboratories.

The materials have demonstrated performance improvements across more than 20 battery manufacturers and multiple lead-acid battery applications.

Lacs of tubular, motor starting, eRickshaw and VRLA batteries with Cancrie Nanocarbon sold in last two years

# Lead-Acid Battery Manufacturer Instruction Manual

## Cancrie Nanocarbon Paste Mixing Process

Cancrie Nanocarbon is designed to improve battery performance, charge acceptance, cycle life, and sustainability in lead-acid battery systems.

This manual provides guidelines for integrating Cancrie Nanocarbon into lead-acid battery paste mixing processes.

## Maintenance & Care

- Keep in a dry area and away from sunlight.

- Keep away from moisture.

## Paste Mixing Process

- Add Cancrie Nanocarbon at 0.3% by weight of oxide.
For every 100 Kg negative oxide, mix 300 Gms of Cancrie Nanocarbon.

- Add Cancrie Nanocarbon directly as carbon powder to oxide before adding water and sulfuric acid.

- Do not add carbon black, graphite, or any other carbon material.

- Add all other additives as per your existing recipe.
Dry mix all additives with oxide for approximately 15 minutes until uniformity is achieved.

- Add 10–12% more water compared to regular carbon black batches.
If additional water is not added, the expected performance and cycle life improvements may not be achieved.

- Additional water may be added during the later stages of pasting if required.

- Add sulfuric acid as per the existing manufacturing recipe.

- Weight of wet/cured negative plates should be approximately 3–5% lower than regular carbon plates.

## Expected Performance Improvements

This process may provide:

- approximately 75% better negative plate strength

- approximately 5% oxide savings

- approximately 100% carbon black/graphite savings

- higher Ah/Wh efficiency

- improved high-rate charge/discharge performance upon cycling

- approximately 20% better charge acceptance

- approximately 20% longer cycle life

## Recommended Validation Tests

### Plate Drop Test

Expected improvement:

- approximately 50–75% better plate strength

### Charge Acceptance Test

Charge acceptance test at 14.4V for 12V batteries may demonstrate:

- approximately 25–60% higher charge acceptance in SLI batteries

- approximately 20% higher charge acceptance in tubular batteries

# Awards & Recognition

## Energy Transition Innovation Challenge (ENTICE) 2023

Cancrie was recognized as a winner of the Energy Transition Innovation Challenge (ENTICE) 2023 for developing scalable clean energy and sustainable battery material solutions.

The recognition was presented during The Energy Transition Dialogues event attended by Amitabh Kant, G20 Sherpa, Government of India.

## G20 Energy Transition Recognition

Cancrie was featured among clean technology innovators contributing to sustainable energy transition and low-carbon industrial solutions.

The company was recognized for its work in biomass-derived nanocarbon materials for advanced energy storage systems.

## UNIDO-FLCTD Innovation Challenge Winner

Cancrie won the UNIDO-FLCTD Innovation Challenge in the Electrical Energy Storage category.

The program supports innovative technologies focused on commercialization, energy efficiency, and sustainable industrial development.

## Techstars Indy Class of 2021

Cancrie was selected as part of the Techstars Indy Class of 2021 startup accelerator program.

## Biotechnology Ignition Grant (BIG) Recognition

Cancrie was recognized under the Biotechnology Ignition Grant (BIG) startup support ecosystem for innovation-driven deep technology development.

## ACT Grants Support Recognition

Cancrie received support through ACT Grants for the development and advancement of sustainable nanocarbon technologies.

## Heritage Venture Group Portfolio Company

Cancrie was recognized as a portfolio company of Heritage Venture Group for its advanced battery material and clean technology innovations.

## Government of India Seed Grant Recognition

Cancrie received seed grant support for developing patented advanced nanomaterial solutions for energy storage applications.

## Clean Technology & Sustainability Recognition

Cancrie has been recognized for:

- sustainable battery material innovation

- biomass-derived nanocarbon development

- clean energy storage solutions

- circular manufacturing approaches

- reduced carbon footprint technologies

- energy transition support systems

# Technical FAQs

## General Technology

### What is Cancrie Nanocarbon?

Cancrie Nanocarbon is a biomass-derived advanced nanocarbon material designed to improve battery performance, efficiency, conductivity, and cycle life.

### What makes Cancrie different from conventional carbon materials?

Cancrie Nanocarbon provides improved conductivity, enhanced active material bonding, better charge acceptance, lower internal resistance, and longer battery life compared to conventional carbon black materials.

### Is Cancrie Nanocarbon biomass-derived?

Yes. Cancrie Nanocarbon is produced using biomass-derived feedstock instead of fossil-fuel-derived carbon materials.

### Why is biomass-derived nanocarbon important?

Biomass-derived nanocarbon helps reduce fossil dependency, lowers lifecycle emissions, and supports sustainable battery manufacturing.

### Does Cancrie reduce battery manufacturing carbon footprint?

Yes. Cancrie helps reduce supply-chain-related CO₂ emissions by replacing petroleum-derived carbon materials with biomass-derived nanocarbons.

## Charge Acceptance & Fast Charging

### What is charge acceptance in a battery?

Charge acceptance refers to a battery’s ability to efficiently absorb and store electrical energy during charging.

### Why is charge acceptance important?

Higher charge acceptance enables faster charging, lower energy loss, improved efficiency, and better battery performance during repeated charging cycles.

### What causes poor charge acceptance in lead-acid batteries?

Poor conductivity, sulfation, high internal resistance, and inefficient ion transport can reduce charge acceptance.

### How does Cancrie improve charge acceptance?

Cancrie Nanocarbon improves conductivity, pore structure, ion transport, and active surface utilization within the negative plate.

### What charge acceptance improvements have been observed?

Testing demonstrated up to 60% higher charge acceptance in lead-acid battery systems.

### Does Cancrie support fast charging?

Yes. Cancrie Nanocarbon demonstrated stable charging performance up to 0.22C charging rates without material degradation.

## Sulfation & Battery Life

### What is sulfation in lead-acid batteries?

Sulfation occurs when lead sulfate crystals accumulate on battery plates, reducing charging efficiency and battery performance.

### How does Cancrie reduce sulfation?

Cancrie Nanocarbon improves charge acceptance, conductivity, and ion mobility, reducing sulfation formation during repeated cycling and partial-state-of-charge operation.

### Does Cancrie improve battery cycle life?

Yes. Improved conductivity, reduced sulfation, and stronger active material bonding contribute to longer cycle life.

### What cycle life improvements have been observed?

Deep discharge testing demonstrated approximately 20–25% improvement in cycle life depending on battery application and operating conditions.

### Does Cancrie improve deep discharge performance?

Yes. Cancrie Nanocarbon supports improved performance during repeated deep discharge cycling conditions.

## Lead-Acid Battery Manufacturing

### Is Cancrie compatible with existing manufacturing systems?

Yes. Cancrie Nanocarbon is designed as a drop-in compatible solution requiring no major equipment modifications.

### Does Cancrie require process redesign?

No. The material integrates into existing paste mixing and battery manufacturing workflows.

### Is carbon black still required?

No. Cancrie Nanocarbon is designed to replace conventional carbon black and graphite additives.

### What is the recommended dosage?

Recommended dosage is approximately 0.3% by weight of oxide.

### Is additional water required during paste mixing?

Yes. Approximately 10–12% additional water compared to regular carbon black batches is recommended.

### Does Cancrie improve plate strength?

Yes. The nanocarbon structure improves active material cohesion and negative plate strength.

### Does Cancrie reduce plate shedding?

Yes. Improved structural integrity helps reduce negative plate shedding during cycling and vibration conditions.

## Automotive & Start-Stop Batteries

### Why are automotive lead-acid batteries challenging?

Automotive batteries operate under high temperatures, vibration, repeated short charging cycles, and frequent engine restarts.

### How does Cancrie help start-stop batteries?

Cancrie improves conductivity, charge recovery, thermal stability, vibration resistance, and sulfation resistance.

### Does Cancrie improve vibration resistance?

Yes. Reinforced active material structure improves resistance to vibration and mechanical stress.

### Does Cancrie increase water loss?

No. Cancrie Nanocarbon is designed to maintain thermal stability without accelerating water loss.

### Is Cancrie suitable for hot climates?

Yes. The material is designed for stable operation under high-temperature battery environments.

## Solar & Stationary Energy Storage

### Why are solar batteries difficult to operate?

Solar batteries frequently experience partial-state-of-charge operation, deep discharge cycles, irregular charging conditions, and temperature fluctuations.

### How does Cancrie improve solar battery performance?

Cancrie improves charge acceptance, reduces sulfation, supports PSOC operation, and improves recharge efficiency during low sunlight conditions.

### Does Cancrie improve renewable energy storage systems?

Yes. Improved charging efficiency and cycle stability support more reliable renewable energy storage performance.

### Does Cancrie improve off-grid energy reliability?

Yes. Improved battery efficiency and longer cycle life help deliver more stable off-grid energy performance.

## Lead-Oxide & Material Efficiency

### How does Cancrie help reduce lead-oxide dependency?

Cancrie Nanocarbon can reduce overall lead oxide requirement through improved electrochemical efficiency and material utilization.

### How does reduced lead usage benefit manufacturers?

Reduced lead usage can lower raw material exposure, reduce cost volatility risk, and improve sustainability metrics.

### Does Cancrie improve energy efficiency?

Yes. Improved conductivity and electrochemical efficiency contribute to higher Ah and Wh efficiency.

### What efficiency improvements have been observed?

Testing demonstrated up to 98% Ah efficiency and up to 85% Wh efficiency.

## Thermal & Structural Performance

### Does Cancrie reduce internal resistance?

Yes. The engineered nanocarbon structure improves conductivity and reduces internal resistance.

### Why is lower internal resistance important?

Lower internal resistance improves charging efficiency, reduces heat generation, and supports safer battery operation.

### Does Cancrie improve thermal stability?

Yes. Improved conductivity and heat distribution support better thermal stability during operation.

### Does Cancrie help prevent thermal runaway?

Improved thermal and electrical conductivity may help reduce localized heat buildup within the battery.

## Material Science & Processing

### Why does Cancrie focus on material behavior?

Cancrie follows a material-first engineering approach where process design is optimized around material properties and particle behavior.

### What material properties are important in battery materials?

Important properties include:

- particle size distribution

- density behavior

- morphology

- surface interaction

- conductivity

- porosity

### Why is material behavior important in industrial processing?

Material behavior directly impacts process stability, product consistency, efficiency, and long-term manufacturing reliability.

### Does Cancrie support scalable manufacturing?

Yes. Cancrie materials and processes are designed for scalable industrial manufacturing integration.

## Validation & Testing

### Has Cancrie been validated by third-party laboratories?

Yes. Testing has been validated by ARAI and third-party accredited laboratories.

### Which tests have been performed?

Validation includes:

- charge acceptance testing

- deep discharge cycling

- FESEM analysis

- Ah/Wh efficiency testing

- vibration testing

- high-rate charging evaluation

### Has Cancrie been tested under industry standards?

Yes. Testing has been conducted under IEC 60095 and BIS:14257 protocols for automotive battery applications.

### Has Cancrie been used in industrial-scale production?

Yes. Cancrie Nanocarbon has been deployed in large-scale battery manufacturing environments.